## Slide 1
Introduction to Fuel Cell Systems
Linnéa Strandberg
Department of Physics
Chalmers University of Technology Göteborg, Sweden

## Slide 2: Learning outcomes
What a fuel cell is – fundamental principles and motivation
(a bit of) Electrochemistry
Electrode reactions, potentials, and current
Thermodynamics, efficiency and losses
Fuel cell components
Principles of components in the fuel cell system
Electrochemical testing and evaluation

## Slide 3: What is a fuel cell?
A Fuel Cell is a “factory” that converts chemical energy (fuel) to electricity (and heat). Delivers electricity as long as fuel is supplied (continuous operation).
An example, the H2-O2 fuel cell:
H2 + ½O2 → H2O
Chemical Energy → Electrical Energy

## Slide 4: What is a fuel cell?
Many types of fuel cells
PEMFC:
Part of a sustainable energy system
Using Hydrogen as energy carrier
Similar to batteries, however FCs can run as long as fuel is provided externally
FCs have longer ranges, higher energy densities and faster refueling times as compared to battery technology
H2 + ½O2 → H2O

## Slide 5: How does a fuel cell work?
A chemical combustion reaction:
Burning of Hydrogen:
(H = -285.8 kJ/mol)
Combustion:
1.
2.
Molecules collide (H2 and O2) Bonds are broken/formed
H-H and O-O bonds are broken
H-O bonds are formed
Redistribution of electronic charge
Product is formed
3.
Takes place on the order of ps (10-12)
Energy difference is released as heat

## Slide 6: How does a fuel cell work?
Anode
Cathode
e- 
H+
Separating reactions allows us to use electrons to perform work before they are recombined
Separate reactions in space!
Hydrogen oxidation reaction
Oxygen reduction reaction

## Slide 7: Fuel Cell History
1838/1839 Both Christian Friedrich Schönbein and William Robert Grove described the effect of fuel cell operation.
“Two strips of platinum 2 inches long and three-eighths of an inch wide, standing erect at a short distance from each other, passed, hermetically sealed, through the botton1 of a bell glass; the projecting ends were made to communicate with a delicate galvanometer; the glass was filled with water acidulated with sulphuric acid”
“The instant the tubes were lowered so as to expose part of the surfaces of platinum to the gases, the galvanometer needle was deflected so strongly as to turn more than half round : it remained stationary at 15°, the platinum in the hydrogen being similar to the zinc element of the pile.”
“After 24 hours, the water had risen half an inch in the tube containing hydrogen, and three eighths of an inch in that containing oxygen.” Grove, Phil. Mag. S. 3. Vol. 14. No. 86, Feb. 1839.
1842 William Robert Grove demonstrated that connecting cells in series produced a potential that could split water.
Grove, Phil. Mag. S. s. Vol. 21. No. 140. Dec. 1842.

## Slide 8: Fuel Cell History
1932-60 – Alkaline Fuel Cells, used in NASA’s Apollo space program. 1960-90 – First PEM Fuel Cell, used in the Gemini space program, Submarines etc.
1960 – Fuel cell powered tractor
1990 – Road test with Fuel Cell busses. Increased research
2000-2010 – Large technical improvements, new applications, promising tests, automotives, backup, portable power, etc.
2008 – “the year that fuel cells became true consumer products”
2013 – First commercial passenger cars

## Slide 9: Thermodynamics
Maximum potential (all work is electrical work):
For hydrogen fuel cell:
Gibbs free energy:
Constant temperature and pressure:
Electrical work done by cell:
n electrons transfered in process,
F faraday constant (charge per mole electrons)
E cell potenital
Maximum work possible in a chemical process
Efficiency
@ Standard state (25 °C and 1 bar)

## Slide 10: Efficiency limit of Fuel Cells
0
200
800
1000
0.3
0.2
0.4
0.5
0.6
0.7
0.8
0.9
1
400 600
Operating Temperature [ o C]
Efficiency,
ε
FC, liquid product
FC, steam product
Carnot limit, 50 o C exhaust
Theoretical limit
100% efficiency  E = 1.48 V
(No heat loss)
Operating efficiency ε = E
1.48

## Slide 11: Losses
Real efficiency
(Not included losses
of unused fuel)

## Slide 12: PEMFC structure

## Slide 13: Catalyst layer/Electrodes
Where the reactions happens
Catalyses reactions, speed up process
Industry standard Pt/C
Catalyst Pt:
High activity
Small nanoparticles  large surface area
Carbon support:
High surface area, support Pt
Porous structure (gas transport)
electrically conductive
Ionomer:
Allows for ion transport (H+ ions)
Tripple phase boundary:
Physical location/phase boundary where
Oxygen, H+ ions and electrons can react

## Slide 14: Proton exchange membrane
Separates half reactions
Conducts ions (H+) from anode to cathode
Prevents gas crossover
Electrically insulating
Ionomer: ion conductive polymer

## Slide 15: Gas diffusion layer
Distributes gases
Electrically conductive
(Some) mechanical stability
Often carbon cloth or carbon paper
with microporous layer (MPL)
Water management  MPL PTFE treated

## Slide 16: Membrane electrode assembly
CCM: membrane with anode and cathode catalyst layer coated on either side
CCM + GDL held together with gaskets
Sandwiched between flow fields and current collecors

## Slide 17: The Fuel Cell Stack
2022-01-21
37
Many Fuel Cells are connected in series to form a “stack”
From the stack: Current depends on the area of the electrode in one cell Voltage depends on the number of cells connected in series Power = Current ∙ Voltage

## Slide 18: Surrounding system
+ Heating (not shown here)

## Slide 19: Electrochemical protocol
Activation procedure
Recovery
Cyclic voltammograms (CVs)
  Characterize the surface
  ECSA
Polarisation curves
  Characterise performance
Accelerated stress test
  Simulate ’real-life’ degradation in a shorter time period

## Slide 20: Electrochemical methods
Activation
  Potenital hold at
    0.6 V for 45 min
    0.95 V for 5 min
    0.85 V for 10 min
Recovery
  Potential hold at 0.2 V for 2 h
X 10
  Increases performance
  Remove/reducing impurities and contaminants from production
  Changes membrane morphology
  Recovers reversible losses
  Reduces contaminants
  H2/Ar
  80 °C
  100% RH
  H2/Ar
  60 °C
  100% RH

## Slide 21: Electrochemical methods
Cyclic voltammetry (CV)
  Potential scan
    From 0.07 V to 1.0 V
    50 mV/s
  Study redox reactions and electrochemical behaviour of electrode and electrolyte.
  Measure electrochemical surface area
  H2/Ar
  40 °C
  100% RH

## Slide 22: CV of Pt in acid

## Slide 23: Electrochemical surface area (ECSA)
Often used in
fuel cell research:
Total charge:
ECSA:
Where
L is surface load (0.4 mg/cm2)
A is electrode area (5 cm2)
Surface charge of a full H+ layer on polycrystalline Pt
Deduct charge from double layer

## Slide 24: Electrochemical methods
Polarisation curves
  CV
  H2/O2 at anode/cathode
  Study reaction kinetics
  Gives which overpotential is needed to reach a specific current density

## Slide 25: Electrochemical methods
Accelerated stress test
  Increases degradation processes
  Different ASTs aimed at different operation conditions
  Potential hold, potential cycling, RH cycling, temperature cycling etc